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	Conception éléments  batteries
	




Configurations Batteries Série L

	Gamme
	Type batterie 
	Polarité
	Type plaque positive
	Type plaque négative
	Conception élément
	Epaisseur enveloppe
	Plaque enveloppé 

	


Power

	L1B 
	D
	PB+
	PB-
	4 Pos /4 Neg
	1.2
	Positive

	
	L1
	D
	PB+
	PB-
	4 Pos /4 Neg
	1.2
	Positive

	
	L2B
	D
	PB+
	PB-
	5 Pos /5 Neg
	1.2
	Positive

	
	L2 
	D
	PB+
	PB-
	5 Pos /5 Neg
	1.2
	Positive

	
	L3B
	D
	PB+
	PB-
	6 Pos /6 Neg
	1.2
	Positive

	
	L3
	D
	PB+
	PB-
	6 Pos /6 Neg
	1.2
	Positive

	
	L5
	D
	PB+
	PB-
	8 Pos /8 Neg
	1.2
	Positive

	

Premium 
	L1B 
	D
	PB+
	PB-
	4 Pos /5 Neg
	1.2
	Positive

	
	L1
	D
	PB+
	PB-
	4 Pos /5 Neg
	1.2
	Positive

	
	L2B
	D
	PB+
	PB-
	5 Pos /6 Neg
	1.2
	Positive

	
	L2 
	D
	PB+
	PB-
	5 Pos /6 Neg
	1.2
	Positive

	
	L3B
	D
	PB+
	PB-
	6 Pos /7 Neg
	1.2
	Positive

	
	L3
	D
	PB+
	PB-
	6 Pos /7 Neg
	1.2
	Positive

	

Smart
	L1 
	D
	PB+
	PB-
	5 Pos /5 Neg
	1.0
	Positive

	
	L2
	D
	PB+
	PB-
	6 Pos /6 Neg
	1.0
	Positive

	
	L3
	D
	PB+
	PB-
	7 Pos /7 Neg
	1.0
	Positive

	
	L5 
	D
	PB+
	PB-
	9 Pos /9 Neg
	1.2
	Positive

	
	L6
	D
	L100+
	L100-
	10 Pos /10 Neg
	1.2
	Positive

	HD
	L2
	D
	PB+T
	PB-T
	5 Pos /6 Neg
	1.3LV
	Positive

	
	L3
	D
	PB+T
	PB-T
	6 Pos /7 Neg
	1.3LV
	Positive



Configurations Batteries Série M et Série J


	Gamme
	Type batterie 
	Polarité
	Type plaque positive
	Type plaque négative
	Conception élément
	Epaisseur enveloppe
	Plaque enveloppé 

	


Jumpo

	M14
	G
	PM+SP
	PM-
	8 Pos /9 Neg
	1.2
	Positive

	
	M15
	G
	PM+SP
	PM-
	9 Pos /10 Neg
	1.2
	Positive

	
	M15 S
	G
	PM+SP
	PM-
	11 Pos /12 Neg
	1.2
	Positive

	
	M16
	G
	B14+
	B13-
	12 Pos /13 Neg
	1.2
	Positive

	
	M14 MF
	G
	PM+SP
	PM-
	9 Pos /10 Neg
	1.2
	Positive

	
	M15 SMF
	G
	PM+SP
	PM-
	11 Pos /12 Neg
	1.2
	Positive

	
	M16 MF
	G
	B14+
	B13-
	13 Pos /14 Neg
	1.2
	Positive

	Marine
	MAR200
	G
	B14+
	B13-
	13 Pos /14 Neg
	1.3LV
	Positive

	
Power
	M10
	G
	PM+
	PM-
	5 Pos /5 Neg
	1.2
	Positive

	
	M11
	G
	PM+
	PM-
	7 Pos /7 Neg
	1.2
	Positive

	
	M12
	G
	PM+
	PM-
	7 Pos /7 Neg
	1.2
	Positive

	

Premium
	M10
	G
	PM+SP
	PM-
	5 Pos /5 Neg
	1.2
	Positive

	
	M10B
	D
	PM+SP
	PM-
	5 Pos /5 Neg
	1.2
	Positive

	
	M11
	G
	PM+
	PM-
	7 Pos /8 Neg
	1.2
	Positive

	
	M12
	G
	PM+
	PM-
	8 Pos /8 Neg
	1.2
	Positive

	
	MF110
	D
	PM+
	PM-
	8 Pos /9 Neg
	1.2
	Positive

	HD
	M10
	G
	PM+T
	PM-T
	5 Pos /6 Neg
	1.2
	Positive

	
	M11
	G
	PM+T
	PM-T
	7 Pos /8 Neg
	1.2
	Positive





Configurations Batteries Série Asiatiques



	Gamme
	Type batterie 
	Polarité
	Type plaque positive
	Type plaque négative
	Conception élément
	Epaisseur enveloppe
	Plaque enveloppé 

	


Premium

	Ns40
	D
	E115+
	E115-
	4 Pos /5 Neg
	1.0
	Positive

	
	Ns60
	D/G
	E115+
	E115-
	5 Pos /6 Neg
	1.0
	Positive

	
	D23
	D
	B14+
	B13-
	4 Pos /5 Neg
	1.2
	Positive

	
	D26
	D/G
	PM+
	PM-
	5 Pos /6 Neg
	1.2
	Positive

	
	D31
	D/G
	PM+
	PM-
	7 Pos /8 Neg
	1.2
	Positive
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